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Tw71 Polymer Modified
Cementitious Waterproofing 
                                                  DS-EN-TW71-0726

PRODUCT NAME

TW71 Polymer Modified Cementitious Waterproofing
COLOR

Grey 
Manufacturer

TM Building Materials Pvt. Ltd.
Plot No.416, FIE, Patparganj Industrial Estate, Delhi-110092, India
Tel: +91-11-43020132
Website: www.thmaterials.com
Product description
TW71 is a two-component polymer modified cementitious waterproofing coating. The product has been designed to be mixed on-site, applied to substrate. It eventually cures to form an elastomeric impermeable waterproofing membrane. 

FEATURES AND BENEFITS

· Non-hazardous, safe 

· Easy to use

· Excellent bond strength

· Flexible, can cover small crack

· Excellent weather and water resistance

USES

· Kitchens and laundries

· Bathroom (tub surrounds, showers, shower pans)

· Balconies, decks and basements

· Interior and exterior

· Pools

· Dry or wet areas

SUITBLE SUBSTRATES

· Concrete

· Masonry (cement block or brick)

· Cured cement mortar beds

· Cement backer boards

PACKAGING

66kg/set (20kg/pail+2*23kg/bag)
10kg/pail
5kg/pail
APPROXIMATE COVERAGE

1.3 – 1.5kg/m2/mm
SHELF LIFE
Storage temperature range between 5℃ and 35℃, in dry and cool area, the product shelf life in factory sealed containers is 12 months..

* High humidity will reduce the shelf life of bagged products.
LIMITATIONS AND CAUTIONS

· Should not be used when the temperature is below 5℃.
· The product must be finished within one hour after mixed.

· Once material is cured, water or liquid should not be added for re-mixing.
· The membrane MUST be protected with other finishing.
· Must straightly follow manufacturer’s written instructions.
· The product contains cement that is stimulus to eyes and the skin, necessary protection tools (clothes) are needed during installation. In case of splashing to the eyes, clean with sufficient water and go to see the doctors when necessary. 
· The freshly applied coating should be protected from rain and strong wind until dry to the touch.
· Keep out of reach of children.

TECHNICAL DATA 

Physical Properties
(Meets or exceeds GB/T23445-2009 Ⅲstandard.)
	Test
	Specification (Type Ⅲ)
	Test 

Result

	Solid Content /%
	≥70
	81

	Tensile Strength

/MPa
	Without Treatment
	≥1.8
	3.0

	
	Retention rate after heat treatment %
	≥80
	117

	
	Retention rate after alkali treatment %
	≥70
	120

	
	Retention rate after water immersion %
	≥70
	103

	Breaking Elongation Rate %

/MPa
	Without Treatment
	≥30
	31

	
	Heat Treatment
	≥20
	30

	
	Alkali Treatment
	≥20
	30

	
	Water Immersion
	≥20
	30

	Low Temperature Flexibility（Φ10mm bar）
	-
	-

	Bond Strength

/MPa 
	Without Treatment
	≥1.0
	1.6

	
	Damp Surface
	≥1.0
	1.5

	
	Alkali Treatment
	≥1.0
	1.6

	
	Water Immersion
	≥1.0
	1.6

	Water Impermeability（0.3MPa，30min）
	Imper-

meability
	Imper-

meability

	Impermeability（mortar negative side）/MPa                  
	≥0.8
	1.5


APPLICATION
1) Surface Preparation

All surfaces must be sound, clean, free of oil, wax, frost, curing agents, form release agents or other inhibiting contaminants, before application of TW71 Polymer Modified Cementitious Waterproofing. Typically, concrete surfaces can be cleaned using a high pressure water jet.

No cracking at the corner nor at the pipe root.

2) Mixing
Based on the mixing ratio powder: liquid = 2.3:1 (weight ratio), carefully pour the liquid into a clean mixing container and slowly add the powder. Mix with a low-speed mixer (about 350rpm) to a smooth, creamy paste consistency. Allow the material to slake in the container for 10 minutes and remix for about 3 minutes.

3) Application
Apply mixed materials evenly on the surfaces for at least two times. The first coat should be applied at a wet film thickness of 0.5mm along the horizontal direction. Allow first coat to cure for 2 to 4 hours. The first coat should be left dry to the touch. The second coat should also be applied at a wet film thickness up to 1.5mm along the vertical direction.
Availability and price

availability
TAMMY products are available worldwide.

For distributor information:

Tel: +91-11-43020132
Email: india@thmaterials.com

Price

Contact a TAMMY representative / Authorized dealer in your area.

Technical service

TECHNICAL ASSISTANCE

Information is available by calling the TAMMY Technical Service at:


Tel: +91-11-43020132
Email: india@thmaterials.com

Ds and msds
DS and MSDS are available on TAMMY website: www.thmaterials.com
TM Building materials PVT. ltd.
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The datasheet is subject to change without notice. For the latest version, visit www.thmaterials.com

